## Slide 1: Simulating Changes in Raman Spectra of Point Defects in UO2 from Lattice Dynamics
Eugene J. Ragasa1
Aleksandr Chernatynskiy1
Simon R. Phillpot1
1Materials Science and Engineering
University of Florida

## Slide 2: Motivation for Studying Raman UO2 point defects
UO2 is the primary fuel in current nuclear reactors
In-reactor operation causes irradiation damage:
  Chemical changes
  Atomic displacements
Off-stoichiometry due to accommodation of O[1]
Characterization of defects
[1] He et al. Phys. Chem Chem. Phys. 12 (2010) 8109-8118
Fig 1. Irradiated UO2 with Raman spectra of different grains[1]
Notes: UO2 a fluorite structure. Group theory predicts 3 frequency modes
278 cm-1 (3xF1uIR active), 445 cm-1 (2xT2g) and 578 cm-1 (F1u).

## Slide 3: Vibrational Spectroscopy
Infrared (IR) Spectroscopy
Light is absorbed
Change in dipole moment
Raman Spectroscopy
Light is scattered
Change in polarizability
Energy-level diagram showing the states involved in Raman signal. [2]
[2] Wikipedia. “Raman spectroscopy.” http://en.wikipedia.org/wiki/Raman_spectroscopy. Accessed June 11, 2014.

## Slide 4: Raman Characterization of UO2 defects
Irradiation-induced defects[3]
25 MeV He ions
U1, U2, U3 compared to U4O9
Proposed to correspond to
  O vacancies
  O interstitials
Changes in Raman Spectrum should be interpreted by symmetry breaking arguments
[3] Guimbretiere, et al. Appl. Phys. Lett. 103, 251914 (2012)

## Slide 5: Raman Spectra Simulation Strategy
Eigenvalues and Eigenvectors of dynamical matrix
From calculation of phonon density of states[5]
Calculated using lattice dynamics
Numerical derivatives of 3rd Order Polarization tensor
Calculated from modern theory of polarization[6]
Calculated from density functional theory methods
Intensity gives height of the Raman peak[4]
[4] Wood, RF. "Lattice Dynamics and Related Properties of Point Defects." Vibrational Properties of Solids 15 (1976): 119-162.
[5] Born, Max, and Kun Huang. Dynamical theory of crystal lattices. Vol. 188. Oxford: Clarendon Press (1954).
[6] King-Smith, R. D., and David Vanderbilt. "Theory of polarization of crystalline solids." Physical Review B 47.3 (1993): 1651.

## Slide 6: Process Flowchart
DFT with EFIELD
Ionic Relaxation
Phonon Calculations
Interatomic forces
Phonon Frequencies and Modes
Relaxed atomic positions
Calculate Raman Signature
Get Raman Tensor
Get Raman Intensity
Determine Raman Signature
[7] Umari et al, Diamond and related materials 14.8 (2005): 1255-126

## Slide 7: Simulation Results
Calcium fluorite
  Same fluorite structure as UO2
  Simpler electronic structure
Structures
  CaF2, ideal crystal
  CaF2 with fluorine vacancy
  CaF2 with Frankel defect
UO2 Structures
  UO2 ideal crystal
  UO2 with oxygen vacancy

## Slide 8: Computational Raman Spectra on CaF2 with point defects
new peaks due to point defects
peak broadening

## Slide 9: Raman Spectra on Damaged CaF2
Change in spectra due to laser induced damage
[8] Bauer, et al. Optics Express. 17.10 (2009), 8253

## Slide 10: UO2 DFT Computational Details
Spin polarized calculations
+U correction for strongly correlated 5f elections
    Creates multiple metastable phases (local minima)
    Difficult to calculate ground state
    Occupation Matrix Control[9]
Approximations
    collinear antiferromagnetic order / paramagnetic order
    antiferromagnetic assumption causes z-axis compression
    use average lattice constants (a=b=c)
[9] Dorado, et al, Phys. Rev. B, 79:235125, 2009

## Slide 11: Simulated Raman Spectra on UO2 with O vacancy

## Slide 13: Raman Spectra on Irradiated UO2
Change in Raman Spectra due to irradiation
[10] Desgranges, Raman spectrum of U4O9: a new interpretation of J. Raman Spectrosc., 43 (2012) 455–458.

## Slide 14: Conclusion
Results:
Calculation of Raman signature for ideal crystals in CaF2 and UO2
  Agreement with experimental data
Calculation of Raman signature for anion defects
  Creation of new Raman peaks agrees with irradiation damage observations
Follow-on work:
Analysis of vibrational modes
  Mode localization of new Raman active modes
  Shift of original Raman mode
Other defect structures
  Charged defect structures (interstitials)
  Oxygen defect density
UO2 DFT convergence of electronic structures
  applied electric fields
  U lattice vacancies and substitutions
Questions: Eugene Ragasa, eragasa@ufl.edu

## Slide 15: Acknowledgements

## Slide 16: Polarization Tensor
[12] Umari, P., and Alfredo Pasquarello. "Infrared and Raman spectra of disordered materials from first principles." Diamond and related materials 14.8 (2005): 1255-126
Raman Cross-section:
Raman Tensor:
Change in Polarization:

## Slide 17: Raman scattering

## Slide 18: Calculation of Raman Tensor
Raman Cross-section is
Elements of the Raman tensor
Associated with the eigenvectors
Derivative of dielectric susceptibility tensor w.r.t atomic position

## Slide 19: Numerical Procedure
Calculate derivatives of dielectric susceptibility as derivatives of force w.r.t finite electric fields
Numerical derivatives
Diagonal elements
Cross-elements:

## Slide 20: Calculation of Polarization Tensor
CaF2_01 0.00000 0.00000 0.00000
CaF2_02 -0.00200 0.00000 0.00000
CaF2_03 -0.00100 0.00000 0.00000
CaF2_04 0.00100 0.00000 0.00000
CaF2_05 0.00200 0.00000 0.00000
CaF2_06 0.00000 -0.00200 0.00000
CaF2_07 0.00000 -0.00100 0.00000
CaF2_08 0.00000 0.00100 0.00000
CaF2_09 0.00000 0.00200 0.00000
CaF2_10 0.00000 0.00000 -0.00200
CaF2_11 0.00000 0.00000 -0.00100
CaF2_12 0.00000 0.00000 0.00100
CaF2_13 0.00000 0.00000 0.00200
CaF2_14 0.00100 0.00100 0.00000
CaF2_15 0.00100 -0.00100 0.00000
CaF2_16 -0.00100 0.00100 0.00000
CaF2_17 -0.00100 -0.00100 0.00000
CaF2_18 0.00100 0.00000 0.00100
CaF2_19 0.00100 0.00000 -0.00100
CaF2_20 -0.00100 0.00000 0.00100
CaF2_21 -0.00100 0.00000 -0.00100
CaF2_22 0.00000 0.00100 0.00100
CaF2_23 0.00000 0.00100 -0.00100
CaF2_24 0.00000 -0.00100 0.00100
CaF2_25 0.00000 -0.00100 -0.00100